## Slide 1: Modeling the phase transformation which controls the mechanical behavior of a protein filament
Peter Fratzl
Matthew Harrington Dieter Fischer
Potsdam, Germany
108th STATISTICAL MECHANICS CONFERENCE
December 2012

## Slide 2
mussel
byssus
whelk egg
capsule
Relatively high initial stiffness
400 MPa
100 MPa
1) Stiffness
important yield
important yield
2) Extensibility
slow
immediate recovery
3) Recovery

## Slide 4
Mussel byssal threads
Self-healing fibres

## Slide 5
yield
relaxation
„healing“ ~ 24h
Mechanical function of Zn – Histidine bonds
M. Harrington et al, 2008
elastic
1h

## Slide 6
Egg capsules
of marine whelk
Busycotypus canaliculatus
Harrington et al. 2012
J Roy Soc Interface

## Slide 7
α-helix
extended β*
α
β*
Raman

## Slide 8
X-ray (small-angle) diffraction

## Slide 9
Raman
intensity
XRD intensity
stress strain
α
β*
Phase coexistence
yield

## Slide 10
Co-existence of two phases during yield
Elastic behaviour
W(s) = (k/2) (s – s0)2

## Slide 11
Force f
actual
length
s
extended
(contour)
length
L
persistence
length
lp
kink
number
ν
length
at rest
s0
Worm-like chain
(Kratky/Porod 1949)
Molecule with kinks
(Misof et al. 1998)
(s > s0)
extended
phase
β*

## Slide 12
Relation between force and potential energy:
β* phase (entropic)
α phase (elastic)
Low strain
High strain
WLC
kink
model

## Slide 13
All molecular segments in the fiber see the same force
fa
mechanical equilibrium:
Complete analogy to thermodynamic equilibrium:

## Slide 14
Total energy
WLC and kink model nearly
identical on this scale
internal
energy
work of
applied force
α stable stability limit α + β*
sclow

## Slide 15
Relation to experiment
What can be measured
(by in-situ synchrotron
x-ray diffraction):
Force as a function of
mean elongation
The critical force at yield
(α-β* coexistence)
The yield point
(start of α-β* coexistence)
Number of molecules
per cross-sectional area
Reconstruct W(s)

## Slide 16
Based on: R. Abeyaratne, J.K. Knowles, Evolution of Phase Transitions – A Continuum Theory (Cambridge University Press, Cambridge, 2006)
Phase transformation kinetics
in analogy to pseudoelasticity in NiTi
thermodynamic driving force
kinetic equation
fraction of β* segments in the fiber
Hypothesis: load at contant stress rate, (loading) and (unloading)

## Slide 17
Slow or fast stretching
Blue:
Red:
Green:
WLC
Equilibrium
line

## Slide 18
mussel
byssus
whelk egg
capsule
Cooperativity of many weak bonds  phase transition